## Slide 1: QCP for stripe order : An organizing principle of cuprates
Louis Taillefer
University of Sherbrooke
Canadian Institute for Advanced Research
Doiron-Leyraud & Taillefer, arXiv:1204.0490
Taillefer, Annual Review of CMP 1, 51 (2010)
arXiv:1003.2972

## Slide 2: Collaborators
Sherbrooke N. Doiron-Leyraud
J. Chang, R. Daou, E. Hassinger, F. Tafti
O. Cyr-Choinière, S. Dufour-Beauséjour, G. Grissonnanche,
F. Laliberté, D. LeBoeuf, S. René de Cotret
Grenoble K. Behnia, L. Malone, I. Sheikin
Toulouse C. Proust, B. Vignolle
Tallahassee L. Balicas, J. Y. Jo, J.-H. Park
Measurements
YBCO UBC D. Bonn, W. Hardy, R. Liang, B. Ramshaw
Eu-LSCO Tokyo S. Pyon, H. Takagi, T. Takayama, Y. Tanaka
Nd-LSCO Texas J.-G. Cheng, J. B. Goodenough, J.-Q. Yan, J.-S. Zhou
Hg-1201 Minneapolis N. Barisic, M. Greven
Samples

## Slide 3: Cuprate superconductors
Questions
Pairing ?
Tc dome ?
Linear-T resistivity ?
Quantum critical point ?
Pseudogap phase ?
Taillefer, Annual Review of CMP 1, 51 (2010) – arXiv:1003.2972

## Slide 4: Organizing principle
Features
Quantum critical point (QCP)
Spin-density-wave (SDW) order
Fermi-surface reconstruction (FSR)
Linear-T resistivity (A)
Superconductivity – Tc dome
A ~ Tc
Doiron-Leyraud & Taillefer, arXiv:1204.0490
Quantum critical point for SDW order

## Slide 5: The Archetype (TMTSF)2PF6
Doiron-Leyraud et al., PRB 80, 214531 (2009)
Organic superconductor

## Slide 6: The Archetype (TMTSF)2PF6
QCP for SDW order
Quantum critical point (QCP)
Spin-density-wave (SDW) order
Fermi-surface reconstruction (FSR)
Linear-T resistivity (A)
Tc dome
A ~ Tc
Questions
Pairing ?
Tc dome ?
Linear-T resistivity ?
Quantum critical point ?
Pseudogap phase ?
Answers
AF spin fluctuations
Phase competition
SF + Pairing correlations
SDW order

## Slide 7: QCP principle : examples
Organic superconductors (TMTSF)2X X = PF6 , ClO4
Electron-doped cuprates PCCO & LCCO
Iron-based superconductors Co-BaFe2As2 & P-BaFe2As2
Hole-doped cuprate Nd-LSCO

## Slide 8: Electron-doped cuprates PCCO & LCCO
Jin et al., Nature 2011
QCP for SDW order
Quantum critical point (QCP)
Spin-density-wave (SDW) order
Fermi-surface reconstruction (FSR)
Linear-T resistivity (A)
Tc dome
A ~ Tc
Hall
Dagan et al., PRL 2004

## Slide 9: Iron-based superconductors BaFe2As2
QCP for SDW order
Quantum critical point (QCP)
Spin-density-wave (SDW) order
Fermi-surface reconstruction (FSR)
Linear-T resistivity (A)
Tc dome
A ~ Tc
Doiron-Leyraud et al., PRB 80, 214531 (2009)

## Slide 10: Iron-based superconductors BaFe2As2
QCP for SDW order
Quantum critical point (QCP)
Spin-density-wave (SDW) order
Fermi-surface reconstruction (FSR)
Linear-T resistivity (A)
Tc dome
A ~ Tc
Nakai et al., PRB 2010
P-doped BaFe2As2

## Slide 11: Iron-based superconductors BaFe2As2
QCP for SDW order
Quantum critical point (QCP)
Spin-density-wave (SDW) order
Fermi-surface reconstruction (FSR)
Linear-T resistivity (A)
Tc dome
A ~ Tc
Pseudogap phase
Onset above TN
Nematic character
Chu et al., Science 2010
FSR
Upturn in Co-Ba122
Downturn in K-Ba122

## Slide 12: Iron-based superconductors BaFe2As2
QCP for SDW order
Quantum critical point (QCP)
Spin-density-wave (SDW) order
Fermi-surface reconstruction (FSR)
Linear-T resistivity (A)
Tc dome
A ~ Tc
Pseudogap phase
Onset above TN
Nematic character
FSR
Upturn in Co-Ba122
Downturn in K-Ba122

## Slide 13: Iron-based superconductors QCP principle
QCP for spin-stripe order
Quantum critical point
Stripe order
Fermi-surface reconstruction
Linear-T resistivity
Tc dome
A ~ Tc
+ Precursor nematic regime

## Slide 14: Hole-doped cuprate Nd-LSCO
QCP for stripe order
Quantum critical point
Stripe order
Fermi-surface reconstruction
Linear-T resistivity
Tc dome
A ~ Tc
Pseudogap phase
Onset above TCO
Daou et al., Nature Physics 2009

## Slide 15: QCP principle
Taillefer, Annual Review of CMP 1, 51 (2010) – arXiv:1003.2972
ORGANIC
CUPRATE
PNICTIDE

## Slide 16: Hole-doped cuprates

## Slide 17: Pnictides QCP principle
QCP for spin-stripe order
Quantum critical point
Spin-stripe order
Fermi-surface reconstruction
Precursor nematic regime
Linear-T resistivity
A ~ Tc
Tc dome

## Slide 18: Hole-doped cuprates QCP principle
QCP for stripe order
Quantum critical point
Stripe order
Fermi-surface reconstruction
Precursor nematic regime
Linear-T resistivity
A ~ Tc
Tc dome

## Slide 19: Hole-doped cuprates QCP & FSR
Quantum oscillations
Hall & Seebeck coefficients
Doiron-Leyraud et al., Nature 2007
Toulouse
LeBoeuf et al., Nature 2007
Laliberté et al., Nature Comm. 2011
Toulouse
Grenoble
Tallahassee
UD: small electron pocket

## Slide 20: Hole-doped cuprates QCP & FSR
Hall & Seebeck coefficients
LeBoeuf et al., Nature 2007
Laliberté et al., Nature Comm. 2011
Toulouse
Grenoble
Tallahassee
UD: small electron pocket
OD: large hole pocket
QCP in between

## Slide 21: Hole-doped cuprates QCP principle
QCP for stripe order
Quantum critical point
Stripe order
Fermi-surface reconstruction
Precursor nematic regime
Linear-T resistivity
A ~ Tc
Tc dome

## Slide 22: Hole-doped cuprates Stripe order
Doiron-Leyraud & Taillefer, arXiv:1204.0490
Laliberté et al., Nature Comm. 2, 432 (2011)
YBCO
Eu-LSCO
NMR: Wu et al., Nature 2011
Stripe order is universal in hole-doped cuprates
Seebeck coefficient
X-ray: Fink et al., PRB 2011

## Slide 23: Hole-doped cuprates QCP principle
QCP for stripe order
Quantum critical point
Stripe order
Fermi-surface reconstruction
Precursor nematic regime
Linear-T resistivity
A ~ Tc
Tc dome

## Slide 24: Hole-doped cuprates Pseudogap phase
T* from resistivity
Doiron-Leyraud & Taillefer, arXiv:1204.0490

## Slide 25: Hole-doped cuprates Pseudogap phase
Nernst coefficient
Doiron-Leyraud & Taillefer, arXiv:1204.0490
Daou et al., Nature 463, 519 (2010)
LeBoeuf et al., PRB 83, 054056 (2011)
Pseudogap phase = Nematic regime

## Slide 26: Hole-doped cuprates QCP principle
QCP for stripe order
Quantum critical point
Stripe order
Fermi-surface reconstruction
Precursor nematic regime
Linear-T resistivity
A ~ Tc
Tc dome

## Slide 27: Hole-doped cuprates Linear-T resistivity
Resistivity
Linear-T resistivity is universal in hole-doped cuprates
N. Doiron-Leyraud et al., arXiv:0905.0964

## Slide 28: Hole-doped cuprates QCP principle
QCP for stripe order
Quantum critical point
Stripe order
Fermi-surface reconstruction
Precursor nematic regime
Linear-T resistivity
A ~ Tc
Tc dome

## Slide 29: Hole-doped cuprates Linear-T resistivity
Resistivity
Correlation between linear-T resistivity and Tc
N. Doiron-Leyraud et al., arXiv:0905.0964
L. Taillefer, Annual Review of CMP 1, 51 (2010) – arXiv:1003.2972
Cooper et al., Science 2009

## Slide 30: Hole-doped cuprates QCP principle
QCP for stripe order
Quantum critical point
Stripe order
Fermi-surface reconstruction
Precursor nematic regime
Linear-T resistivity
A ~ Tc
Tc dome

## Slide 31: Hole-doped cuprates Tc suppression
SC fluctuations
via Nernst signal above Tc
Hc2 decreases with underdoping
Decrease is non-monotonic : Stripe order
J. Chang et al., unpublished

## Slide 32: Hole-doped cuprates QCP principle
QCP for stripe order
Quantum critical point
Stripe order
Fermi-surface reconstruction
Precursor nematic regime
Linear-T resistivity
A ~ Tc
Tc dome

## Slide 33: Hole-doped cuprates Summary
QCP for stripe order
Quantum critical point
Stripe order
Fermi-surface reconstruction
Precursor nematic regime
Linear-T resistivity
A ~ Tc
Tc dome
Doiron-Leyraud & Taillefer, arXiv:1204.0490

## Slide 34: The QCP principle – a universal scenario ?
ORGANIC
e-DOPE CUPRATE
h-DOPED CUPRATE
PNICTIDE

## Slide 35: Thank you.
Doiron-Leyraud & Taillefer, arXiv:1204.0490
Taillefer, Annual Review of CMP 1, 51 (2010)
arXiv:1003.2972